Evaluator Comment (Sample ID: 10020794). Sample run for test data only. New oil.. LUBETRAK OIL ANALYSIS Contact:; MCMO – Muscle Car Motor Oil. Phone:. E-Mail:; Chris Street..; Unit Info: Unit ID; MCMO. Comp Desc; MUSCLE CAR OIL W/ZALT. Lab No.; 70001... Sample Information: Sample ID; Date Taken; Date Rec; Date Rpt; Date Posted; Oil Miles/Hours; Comp Miles/Hours; Fluid Brand/Type; Fluid Changed; Condition. 10020794; 2010/01/06; 2010/01/12; 2010/01/12; 2010/01/14; 0; 0; 20W50; No; NORMAL.. Fluid Physical Properties: Sample ID; VISC40; VISC100; WATER; SOOT; SOLIDS; FUEL; GLYCOL; NITR; OXID; TAN; TBN. 10020794; 179.2; 19.5; <0.00; N/A; N/A; N/A; N/A; <1; <1; 2.92; 8.0.. Spectro Results: Sample ID; FE; CR; PB; CU; SN; AL; NI; AG; MN; SI; B; NA; MG; CA; BA; P; ZN; MO; TI; V; K. 10020794; 0; 0; 0; 0; 0; 0; 0; 0; 0; 1; 0; 0; 981; 72; 5; 1734; 1862; 1219; 0; 0; 0.. Additional Tests: Sample ID; CHANGE. 10020794; N/A.. Historical Comments: Sample ID; Comment. 10020794; (see above under 'Evaluator Comment')..