LUBETRAK OIL ANALYSIS Contact: MCMO – Muscle Car Motor Oil Phone: E-Mail: Chris Street Unit Info: Unit ID MCMO Comp Desc MUSCLE CAR OIL W/ZALT Lab No. 70001 Evaluator Comment (Sample ID: 10020794) Sample run for test data only. New oil Sample Information: Sample ID Date Taken Date Rec Date Rpt Date Posted Oil Miles/Hours Comp Miles/Hours Fluid Brand/Type Fluid Changed Condition 10020794 2010/01/06 2010/01/12 2010/01/12 2010/01/14 0 0 20W50 No NORMAL Fluid Physical Properties: Sample ID VISC40 VISC100 WATER SOOT SOLIDS FUEL GLYCOL NITR OXID TAN TBN 10020794 179.2 19.5 <0.00 N/A N/A N/A N/A <1 <1 2.92 8.0 Spectro Results: Sample ID FE CR PB CU SN AL NI AG MN SI B NA MG CA BA P ZN MO TI V K 10020794 0 0 0 0 0 0 0 0 0 1 0 0 981 72 5 1734 1862 1219 0 0 0 Additional Tests: Sample ID CHANGE 10020794 N/A Historical Comments: Sample ID Comment 10020794 (see above under 'Evaluator Comment')