LUBETRAK OIL ANALYSIS Contact: S & W AUTOMOTIVE TECHNOLOGIES, INC Address: 73 PRICE QUARTERS RD. STE 273 McDONOUGH, GA 30253 USA Phone: 8015017746 E-Mail: zalt.mco@gmail.com Unit Info: Unit ID MCMO 10W30-1 Comp Desc NEW OIL Lab No. 70001 Evaluator Comment (Sample ID: 10052495) New oil. Diagnosis not applicable. Sample Information: Sample ID Date Taken Date Rec Date Rpt Date Posted Oil Miles/Hours Comp Miles/Hours Fluid Brand/Type Fluid Changed Condition 10052495 2010/08/10 2010/08/12 2010/08/12 2010/08/13 N/A N/A 10W30 No NORMAL Fluid Physical Properties: Sample ID VISC40 VISC100 WATER SOOT SOLIDS FUEL GLYCOL NITR OXID TAN TBN 10052495 N/A 11.0 <0.01 N/A N/A N/A N/A <1 <1 3.11 7.9 Spectro Results: Sample ID FE CR PB CU SN AL NI AG MN SI B NA MG CA BA P ZN MO TI V K 10052495 0 0 0 0 0 0 0 0 0 1 0 0 1150 40 0 1581 1818 1422 0 0 5 Additional Tests: 10052495 - N/A Historical Comments: Sample ID Comment 10052495 (see above under 'Evaluator Comment')