Evaluator Comment (Sample ID: 10052495). New oil. Diagnosis not applicable... LUBETRAK OIL ANALYSIS Contact:; S & W AUTOMOTIVE TECHNOLOGIES, INC. Address:; 73 PRICE QUARTERS RD. STE 273 McDONOUGH, GA 30253 USA. Phone:; 8015017746. E-Mail:; zalt.mco@gmail.com..; Unit Info: Unit ID; MCMO 10W30-1. Comp Desc; NEW OIL. Lab No.; 70001... Sample Information: Sample ID; Date Taken; Date Rec; Date Rpt; Date Posted; Oil Miles/Hours; Comp Miles/Hours; Fluid Brand/Type; Fluid Changed; Condition. 10052495; 2010/08/10; 2010/08/12; 2010/08/12; 2010/08/13; N/A; N/A; 10W30; No; NORMAL.. Fluid Physical Properties: Sample ID; VISC40; VISC100; WATER; SOOT; SOLIDS; FUEL; GLYCOL; NITR; OXID; TAN; TBN. 10052495; N/A; 11.0; <0.01; N/A; N/A; N/A; N/A; <1; <1; 3.11; 7.9.. Spectro Results: Sample ID; FE; CR; PB; CU; SN; AL; NI; AG; MN; SI; B; NA; MG; CA; BA; P; ZN; MO; TI; V; K. 10052495; 0; 0; 0; 0; 0; 0; 0; 0; 0; 1; 0; 0; 1150; 40; 0; 1581; 1818; 1422; 0; 0; 5.. Additional Tests: 10052495 - N/A.. Historical Comments: Sample ID; Comment. 10052495; (see above under 'Evaluator Comment')..